This section includes standard commercial Stainless Steel Window Frames and relies on industry standards. This section includes descriptive and performance type specifications. Edit to avoid conflicting requirements.

# General

## SECTION INCLUDES

This article includes a summary of the content of this section which will not be included in other sections. This article is NOT intended to be used as a trade or other form of jurisdictional content.

### [Non-rated] [fire rated] stainless steel window frames.

### [Non-rated] [fire rated] stainless steel panels.

## RELATED SECTIONS

This article references other specification sections that inter-rely on this section. This listing should include those sections that describe subjects or products that affect this section directly.

### Section [______-____________]:  Masonry mortar fill of metal frames.

### Section 07 92 00-Joint Sealing: Caulking between windows and adjacent construction.

### Section 08 81 00 - Glass Glazing: Glazing for installation in stainless steel window frames.

## REFERENCES

Edit this article after editing the rest of this section.  List reference standards that are included within the text of this section, when edited for a project specification.  Delete references that do not apply.

### ASTM A240/A240M-17 - Standard Specification for Chromium and Chromium-Nickel Stainless Steel Plate, Sheet, and Strip for Pressure Vessels and for General Applications.

### Canadian Steel Door Manufacturers Association (CSDMA), Selection and Usage Guide for Steel Doors and Frames, 2009.

### HMMA 802-07 - Manufacturing of Hollow Metal Doors and Frames.

### HMMA 840-16 - Installation and Storage of Hollow Metal Doors and Frames.

### HMMA 841-17 Guide Specifications For Receipt, Storage and Installation of Hollow Metal Doors and Frames.

### NFPA 80-16 - Standard for Fire Doors and Other Opening Protectives.

### UL 10c-16 Standard for Positive Pressure Fire Tests of Door Assemblies

### USGBC – LEED v4.

## REGULATORY REQUIREMENTS

Include the following article only if fire rated assemblies are specified. AMBICO can supply Stainless Steel Window Frames with a 45 minute fire rating label.

### Installed Door and Frame Assembly:  Conform to [NFPA 80] [_________] for fire rated class [as scheduled.] [as indicated.].

## SUBMITTALS

### Product Data:  Provide product data on standard stainless steel window frame construction.

### Shop Drawings:  Indicate stainless steel window frame elevations, internal reinforcement, anchor types and spacing, closure methods, finishes and cut outs [for glazing].

### Samples:  Submit manufacturer's stainless steel finish samples showing range of material variation as well as polishing details.

Include the following ONLY if specifying for a LEED project.  Specify only the technical requirements necessary to achieve the credits desired for this project.  The Type 3 EPD are normally required for LEED v4 certification.  AMBICO stainless steel products offer significant advantages to firms interested in supporting LEED certification.

## Sustainable Design:

### Section 01 35 18:  LEED documentation procedures.

### Provide required LEED documentation for Product.

### Submit Type 3 Environmental Product Declaration (EPD) for Products of this Section.

### iv) 	Manufacturer's Certificate: Certify that Products meet or exceed specified requirements.

## QUALITY ASSURANCE

### Perform Work to requirements of [CSDMA (Canadian Steel Door Manufacturers Association)] [HMA (Hollow Metal Manufacturers Association)] standards.

### Manufacturer:  Minimum 5 years documented experience manufacturing stainless steel window frames.

## DELIVERY, STORAGE AND PROTECTION

### Section [01 61 00]:  Transport, handle, store, and protect products.

### Comply with [CSDMA] [HMMA 840] standards for storage and installation

### Remove window frames from wrappings or coverings upon receipt on site and inspect for damage.

### Store in vertical position, spaced with blocking to permit air circulation between components. Store materials out of water and covered to protect from damage.

## WARRANTY

### Manufacturer's Limited Warranty:  Five (5) years from date of supply, covering material and workmanship.

# Products

## MANUFACTURERS

List the manufacturers acceptable for this project. Edit the subsequent descriptive specifications of Part 2, to identify project requirements and to eliminate any conflict with specified manufacturer's products.

### AMBICO Limited
1120 Cummings Avenue
Ottawa, Ontario, Canada K1J 7R8                                                                                   Toll Free Phone		888-423-2224 
Phone 			613-746-4663                                                                            Toll Free Fax     	800-465-8561
Fax 			613-746-4721

### Other Acceptable Manufacturers:

#### [_____________________________].

#### [_____________________________].

### Substitutions: [Refer to Section 01 60 00.] [Not permitted.]

## MATERIALS

Note: Type #304 stainless steel alloy is standard. Type #316 alloy may be specified for extremely corrosive environments, such as in the presence of chlorine

### Stainless Steel: ASTM A240, type [304] [316].

## ACCESSORIES

The following paragraphs identify the components needed to complement the materials cited above..

### Frame Thermal Breaks:  Rigid polyvinylchloride extrusion.

### Glazing Stops:  Formed stainless steel channel, minimum 16 mm (0.625 inch) high, [butted] [mitred] corners; prepared for countersink style [tamperproof] screws.

### Glass:  [In accordance with Section [08 81 00]] [________]. Glazing to be supplied by others.

## FABRICATION

## Stainless Steel Frames:

#### Stainless Steel Window Frames:  [1.6] [2.0] [2.8] mm ([16] [14] [12] gauge) thick stainless steel, welded type construction, mitred corners.

#### Factory assemble and weld stainless steel window frames.

#### Fabricate with stainless steel hardware reinforcement plates welded in place.

#### Reinforce window frames wider than 1200 mm (48 inches) with roll formed stainless steel channels fitted tightly into frame head, flush with top.

#### Mullions to be fit to perimeter jambs with visible seams in accordance with architectural elevations.

## FINISHES

Edit the following to identify finish. Choose from Standard or Custom finishes.

### Standard Stainless Steel Finish:  [#2B Mill Finish] [#4 Satin] [#6 Hairline] [#8 Mirror] [Colored].

### OR

### Custom Stainless Steel Finish: [Embossed] [Etched] [Patterned] [Non-directional] [Textured] [______]

# Execution

## INSTALLATION

### Install components to manufacturer’s written instructions.

### Install stainless steel window frames to [CSDMA] [HMMA 840] standards [and in accordance with NFPA 80, and local authority having jurisdiction].

### Coordinate with [masonry] [gypsum board] [concrete] [_________] wall construction for anchor placement.

### Set window frames plumb, square, level and at correct elevation.

### Allow for deflection to ensure that structural loads are not transmitted to window frame.

### [Install glazing].

## ERECTION TOLERANCES

### Section 01 73 00: Tolerances.

### Installation tolerances of installed frame for squareness, alignment, twist and plumbness are to be no more then ± 1/16in (1.5mm) in compliance with HMMA 841.

## FIELD QUALITY CONTROL

### .1	Provide qualified manufacturer's representative to instruct installers on the proper installation and adjustment of stainless steel window frames. Correct any deficiencies.

### .2	Provide manufacturer's representative to inspect window frame installation.  Correct any deficient units.

### END OF SECTION